IPS

Innovative Polymer Solutions, Inc.

ATTN:  QUALITY CONTROL

### CERTIFICATION

Product Description			IPS Knit-Tech 9112

Purchase Order No. 			Date			Date of Mfr.

Lot No.					Code No.

Quantity Shipped			Date Shipped

Packaging				No. of Pkgs. Shipped

Shelf Life		THREE MONTHS FROM DATE OF MANUFACTURE

# ]

# NOMINAL COMPOSITION

Knit-Tech 9112 		<60.0  (  5.0

Silica				<35.0  (  5.0

Talc				<10.0  +  5.0

Wax				<5.0    +  5.0

TEST                           REQUIREMENT 	TEST METHOD	RESULTS

# Knit-Tech 9112 Component

Specific Gravity @77(F	1.04  (   0.02		IPS Test  # 01

ASTM-D1298

Color, Gardner		1  -  6			IPS Test # 02

ASTM D2849

pH				5.5  (  1.0		IPS Test # 04

ASTM-E70-52T

Flash Point, (F TCC		100 – 150		IPS Test  # 05

ASTM-D56

Viscosity cps @ 77(F		1000 – 5000		IPS Test # 07

ASTM-D2393 & D1824

# Knit-Tech 9112 Component

Physical Form			Off White Powder	IPS Test #03

% Ash				48.0  (  3.0		IPS Test #11

ASTM-D482

Dispersion Check		Uniform material	IPS Test #38

free of foreign matter

This is to certify that the above shipment has been determined to meet all IPS specification requirements at time of manufacture.

___Peter C. Blyth________________ Technical Director

1002 Foxdale Place Valrico, Florida  33595

Atlanta Office: Ph# 678-240-9224  Fax#  678-240-9225

Tampa Office: Ph# 813-681-2160  Fax#  813-681-2170